## Slide 1
Key West, December 2013
Time-domain observation of coherent phenomena in
solids and nano-structures
Fabrizio Carbone
Ecole Polytechnique Federale de Lausanne
Laboratory for Ultrafast Microscopy and Electron Scattering

## Slide 2
Overview of ultrafast experiments in solids:
- The mechanisms behind phase transitions and the formation of different states of matter.
- Where are these phenomena observable?
- Information in multiple dimensions, static (steady state) and time-resolved.
- How to perform specific excitations in solids.
Examples
- The ISRS mechanism and the coherent oscillations of Cooper pairs.
- Laser-induced uniaxial pressure to probe orbital-ordering or topological transitions
(talk by Luca Piazza).
Perspective, combining tools
- Choose what to excite and where to probe it……….X-ray pump/TEM probe
Outline, overview of LUMES activities

## Slide 3
BCS superconductivity (structurally driven)

## Slide 4
BCS superconductivity (structurally driven)

## Slide 5
Half-filling
Hole doping
O
Cu
ZRS
NB
AB
U=0
B
E
EF
NB
LHB
U>W, Mott insulator
B
E
U
UHB
ECT
ECT = 2 eV
t = 0.3 eV
U = 9 eV
EF
LHB
UHB
NB
ZRS
U
ECT
T
Doping hybridization, splits B
NB
U>ECT, CT insulator
B
E
UHB
U
ECT
LHB
Strongly correlated systems physics (Mott, CT) electronic driven
W. Stephan, and P. Horsch, Phys. Rev. B 42 8736 (1990).

## Slide 6
Fermi liquid
Mazin, Nature 464 (2010)
nodes
antinodes
d-wave order parameter
Fermi liquid
Cuprates phase diagram

## Slide 7
Manganites Jan-Taller, magnetic exchange, spin-orbit (structure+electronic)
M. B. Salamon and M. Jaime, “The physics of manganites: Structure and transport,” Rev. Mod. Phys. 73, 583 (2001).

## Slide 8
Competition between:
CF, J, SO
Tuning:
doping, pressure, magnetic field,
laser light?
Manganites phase diagram
Z. A. Li et al., “A checkerboard orbital-stripe phase and charge ordering transitions in Pr(SrxCa2x)Mn2O7 (0<x<0.45),”
Europhys. Lett. 86, 67010 (2009).

## Slide 9
Many-body absorptions
Bi-magnon
multiphonons….
0.1 eV
CT, Mott gaps
1-2 eV
TM L-edges
300-1000 eV
Energy loss, (eV)
rec.space, (A-1)
K-edges
XANES
EXASF
1-10 keV
Phonons
acoustic
optical
Electronic states
gaps
magnons….
0.01 eV
d-d
1 eV
deeper levels
no dispersion
center of mass
optics
ARPES
EELS
XAS
RXD
XAS
Energy/momentum(rec. space)/intensity diagram of excitations in solids
diffraction

## Slide 10
Energy, (eV)
Real space, (A)
ZL
Plasmons (eV)
core
102 eV
o
A
nm
102 nm
102 μm
μm
TEM
X-ray magnetic
speckle
(X-ray microscopy)
Energy/real-space/intensity diagram of excitations in solids
PRB 88, 014505 (2013)

## Slide 11
X-rays/electrons comparison
"A perspective on novel sources of ultrashort electron and X-ray pulses", F. Carbone, P. Musumeci, O.J. Luiten, C. Hebert, Chemical Physics, 392, 1, (2012)

## Slide 12
Excitation mechanisms
TM L-edges
300-1000 eV
Energy loss, (eV)
rec.space, (A-1)
d-d
1 eV
Excitation processes in solids
Phonons
acoustic
optical
Science 331, 189 (2011);
Many-body absorptions
Bi-magnon
multiphonons….
0.1 eV
PRB 73, 184434 (2006)
Electronic states
gaps
magnons….
0.01 eV
PRL 111, 057002 (2013)
NatComm 2:353 (2011)
CT, Mott gaps
1-2 eV
PRB 82 (2010)
PNAS 110, 4539 (2013)
Direct absorption
THz
Direct absorption
FIR
ISRS
Direct absorption
ISRS
VIS
X-ray excitation:
Direct absorption photodoping
Resonant Raman, chemically
selective excitation
Momentum-resolved
XFEL

## Slide 13
Excitation mechanisms
Example: fs-optical spectroscopy of the coherent oscillation of Cooper pairs
"Evidence for a Peierls phase-transition in a three-dimensional multiple charge-density waves solid."
B. Mansart, M.J.G. Cottet, T. Penfold, S. Dugdale, R. Tediosi, M. Chergui, F. Carbone. PNAS109, 5603 (2012).

## Slide 14
Epump//(110), Eprobe//(110), k//001
F ~ 300 mJ/cm2
A1g+B2g Raman excitation
The signal changes sign as a function of wavelength
Observation of coherent oscillations
Excitation mechanisms
Transient reflectivity in B2g Raman geometry
"Coupling of a high-energy excitation to superconducting quasiparticles in a cuprate from coherent charge fluctuation spectroscopy",
B. Mansart, J. Lorenzana, A. Mahn, A. Odeh, M. Scarongella,M. Chergui, and F. Carbone, PNAS 110, 4539 (2013).
“Investigating pairing interactions with coherent charge fluctuation spectroscopy",
J. Lorenzana, B. Mansart, A. Mann, A. Odeh, M. Chergui, F. Carbone, EPJ 222, 1223-1239, (2013).

## Slide 15
Epump//(110), Eprobe//(110), k//001
F ~ 300 mJ/cm2
A1g+B2g Raman excitation
The signal changes sign as a function of wavelength
The coherent oscillations vanish above Tc
Excitation mechanisms
Transient reflectivity in B2g Raman geometry
"Coupling of a high-energy excitation to superconducting quasiparticles in a cuprate from coherent charge fluctuation spectroscopy",
B. Mansart, J. Lorenzana, A. Mahn, A. Odeh, M. Scarongella,M. Chergui, and F. Carbone, PNAS 110, 4539 (2013).
“Investigating pairing interactions with coherent charge fluctuation spectroscopy",
J. Lorenzana, B. Mansart, A. Mann, A. Odeh, M. Chergui, F. Carbone, EPJ 222, 1223-1239, (2013).

## Slide 16
Epump//(100), Eprobe//(100), k//001
F ~ 300 mJ/cm2
A1g+B1g Raman excitation
The signal changes sign as a function of wavelength
The coherent oscillations vanish above Tc
Excitation mechanisms
Transient reflectivity in B1g Raman geometry
"Coupling of a high-energy excitation to superconducting quasiparticles in a cuprate from coherent charge fluctuation spectroscopy",
B. Mansart, J. Lorenzana, A. Mahn, A. Odeh, M. Scarongella,M. Chergui, and F. Carbone, PNAS 110, 4539 (2013).
“Investigating pairing interactions with coherent charge fluctuation spectroscopy",
J. Lorenzana, B. Mansart, A. Mann, A. Odeh, M. Chergui, F. Carbone, EPJ 222, 1223-1239, (2013).

## Slide 17
Ultrafast experiments compared to static Raman scattering
Excitation mechanisms
FFT of the time-domain signal and the SC gap
"Coupling of a high-energy excitation to superconducting quasiparticles in a cuprate from coherent charge fluctuation spectroscopy",
B. Mansart, J. Lorenzana, A. Mahn, A. Odeh, M. Scarongella,M. Chergui, and F. Carbone, PNAS 110, 4539 (2013).
“Investigating pairing interactions with coherent charge fluctuation spectroscopy",
J. Lorenzana, B. Mansart, A. Mann, A. Odeh, M. Chergui, F. Carbone, EPJ 222, 1223-1239, (2013).

## Slide 18
Ultrafast experiments compared to static Raman scattering
Excitation mechanisms
FFT of the time-domain signal and the SC gap
"Coupling of a high-energy excitation to superconducting quasiparticles in a cuprate from coherent charge fluctuation spectroscopy",
B. Mansart, J. Lorenzana, A. Mahn, A. Odeh, M. Scarongella,M. Chergui, and F. Carbone, PNAS 110, 4539 (2013).
“Investigating pairing interactions with coherent charge fluctuation spectroscopy",
J. Lorenzana, B. Mansart, A. Mann, A. Odeh, M. Chergui, F. Carbone, EPJ 222, 1223-1239, (2013).

## Slide 19
Coupling between photons and
Cooper pairs in the gap region
Yields massive bosons
Excitation mechanisms
Intimate meaning of the gap in SC
PNAS 110, 4539 19 March (2013)

## Slide 20
Excitation mechanisms
Coherent control via chemical selectivity and momentum sensitivity
X-ray pump:
Higher yield for ISRS processes
@ comparable fluence, 10-100
more population of the excited state
Chemical selectivity
tuning excitation energy at resonances
Momentum sensitivity
ability to prepare carriers anywhere in
k-space
“A proposal for fs-electron microscopy experiments on
high-energy excitations in solids.”
Submitted to Micron

## Slide 21
Excitation mechanisms
The highest potential for the excitation, the widest selection for the probe
Tuning the pump
L-edge excitation yields 10-100 times more Bogoliubons
then 1.55 eV excitation at comparable fluence
diffraction
optics
photoemission
Lorentz microscopy
Choosing the probe
Broad search for SC resonance
“A proposal for fs-electron microscopy experiments on high-energy excitations in solids.” Submitted to Micron

## Slide 22
Excitation mechanisms
SC dynamics, photodoping

## Slide 23
Excitation mechanisms
Combine broad probing and pumping range
Energy loss, (eV)
rec.space, (A-1)
TM L-edges
300-1000 eV
d-d
1 eV
Phonons
acoustic
optical
Many-body absorptions
Bi-magnon
multiphonons….
0.1 eV
Electronic states
gaps
magnons….
0.01 eV
CT, Mott gaps
1-2 eV
Direct absorption
THz
Direct absorption
FIR
ISRS
Direct absorption
ISRS
VIS
X-ray excitation:
Direct absorption photodoping
Resonant Raman, chemically
selective excitation
Momentum-resolved
XFEL
Pump:
XFEL
Laser
Many-body absorptions
Bi-magnon
multiphonons….
0.1 eV
CT, Mott gaps
1-2 eV
TM L-edges
300-1000 eV
Energy loss, (eV)
rec.space, (A-1)
K-edges
XANES
EXASF
1-10 keV
Phonons
acoustic
optical
Electronic states
gaps
magnons….
0.01 eV
d-d
1 eV
deeper levels
no dispersion
center of mass
optics
ARPES
EELS
XAS
RXD
XAS
diffraction
Energy, (eV)
Real space, (A)
ZL
Plasmons (eV)
core
102 eV
o
A
nm
102 nm
102 μm
μm
TEM
X-ray magnetic
speckle
(X-ray microscopy)
Probe:
photons
electrons

## Slide 24
Current facilities at LUMES:
- fs optical spectroscopy (40 meV-4 eV, q=0) (Coherent control of SC)
- fs electron diffraction (20 KHz, 105 e-/pulse, 200 fs)
- fs TEM (250 KHz-5 MHz, 350 fs, Lorentz, 1-1000 eV, q dependence)
(Uniaxial pressure effects in a Manganite) L. Piazza et al. Structural Dynamics 1, 1 (2013) Cover.
- fs ARPES (0-1 eV, q dependence, under construction)
EPFL center for ultrafast science (collaboration with prof. Chergui)
- fs X-ray diffraction (200 fs, slicing beamline at PSI)
- fs X-ray absorption spectroscopy (>1000 eV, 200 fs, slicing beamline at PSI)
Perspective experiments:
- XFEL-pump/multidimensional probe (optics, TEM) (under propaganda)
Conclusions:
References:
"Evidence for a Peierls phase-transition in a three-dimensional multiple charge-density waves solid."
B. Mansart, M.J.G. Cottet, T. Penfold, S. Dugdale, R. Tediosi, M. Chergui, F. Carbone. PNAS109, 5603 (2012).
"Design and implementation of a flexible beamline for fs electron diffraction experiments"
G.F. Mancini, B. Mansart, S.Pagano; B. van der Geer,M. de Loos, F. Carbone, Nucl. Instr. Meth. in Phys. Res. A, 691, 113-122 (2012).
"Coupling of a high-energy excitation to superconducting quasiparticles in a cuprate from coherent charge fluctuation spectroscopy",
B. Mansart, J. Lorenzana, A. Mahn, A. Odeh, M. Scarongella,M. Chergui, and F. Carbone, PNAS 110, 4539 (2013).
"Quantitative imaging of flux vortices in the type-II superconductor MgB2 using cryo-Lorentz transmission electron microscopy",
M. Cottet, M. Cantoni, B. Mansart, D. T. L. Alexander, C. Hébert, J. Karpinski, F. Carbone. PRB 88, 014505 (2013). Editors' Suggestion.
"Design and implementation of a fs-resolved transmission electron microscope based on thermionic gun technology",
L. Piazza, D.J. Masiel, T. LaGrange, B.W. Reed, B. Barwick, F. Carbone, Chem. Phys., Volume 423, pp 79-84 (2013).