## Slide 2
outline
temporal pulse
characterization
UED setup and
spatial resolution
lattice dynamics
in graphite

## Slide 3
electron diffraction setup
main parameter:
acc. voltage: 40 kV
acc. field: 11.4 kV/mm
pulse radius: ~ 75 µm
source radius: 2 µm - 30 µm
100 µm
optical white light
microscope image
in reflection
optical white light
microscope image
in transmission
40 keV electron
transmission image
40 keV electron
diffraction pattern
3 nm thin freestanding
single crystalline graphite
preparation with micro-mechanical exfoliation and transfer on Quantifoil® gold TEM-grid
J. C. Meyer et al.,
Appl. Phys. Lett. 92, 123110 (2008)
Notes: setup overview

## Slide 4
electron diffraction setup
8.5 mm cathode-sample distance
electron pulse source
Notes: source in detail
DONT FORGET DETAIL DISCRIPTION!

## Slide 5
Characterization
spatial resolution
electron source size
↔ transerve coherence length
spatial resolution studies
THG pulse beam size
knife edge method
28.0 µm
9.5 µm
2.3 µm

## Slide 6
electron source size
↔ transerve coherence length
spatial resolution
spatial resolution studies

## Slide 7
Femtosecond Spectroscopy and Ultrafast Laser Control
Experimental Physics III
spatial resolution studies
electron source size
↔ transerve coherence length
spatial resolution

## Slide 8
source image expansion
w0 = 28.0 µm
w0 = 9.5 µm
w0 = 2.3 µm
ws = 49 µm
ws = 52 µm
ws = 85 µm
first approximation for transerve coherence length:
xs = 1.1 nm
xs = 3.3 nm
xs = 22.2 nm
transerve coherence length from simulation via emittance:
xs = 1.5 nm
xs = 4.0 nm
xs = 20.4 nm
measured
simulated
spatial resolution studies

## Slide 9
electron sample diffraction
28 µm
9.5 µm
2.3 µm
spatial resolution studies

## Slide 10
, with standard deviation of
van Cittert-Zernike theorem for a Gaussian source
and 88% optical coherence criterium give:
transvere coherence from diffraction data
2D-Gaussian fit
Bragg peak
spatial resolution studies

## Slide 11
mag. lens aberration
detector PSF
deconv. Bragg peak
measured Bragg peak width is a convolution result:
transvere coherence from diffraction data
mag. lens aberration
detector PSF
deconv. Bragg peak
single events
spatial resolution studies

## Slide 12
xi = 1.6 nm
xi = 2.8 nm
xi = 22.7 nm
w0 = 28.0 µm
w0 = 9.5 µm
w0 = 2.3 µm
transvere coherence from diffraction data
spatial resolution studies
deconvoluted
2D Gaussian fit

## Slide 13
temporal pulse
characterization
UED setup and
spatial resolution
lattice dynamics
in graphite

## Slide 14
grating enhanced
ponderomotive scattering
R. J. D. Miller and coworkers,
Optics Express 16, 3334 (2008)
experimental parameters:
energy per pulse: ~ 100 µJ
lens focal length: 300 mm
1/e² focal radius: 33 µm
temporal resolution
temporal resolution studies

## Slide 15
experimental parameters:
energy per pulse: ~ 100 µJ
lens focal length: 300 mm
1/e² focal radius: 33 µm
grating enhanced
ponderomotive scattering
temporal resolution studies

## Slide 16
electron pulse duration at sample position
temporal resolution studies
28.0 µm
9.5 µm
2.3 µm

## Slide 17
temporal pulse
characterization
UED setup and
spatial resolution
lattice dynamics
in graphite

## Slide 18
lattice dynamics in graphite
Notes: setup overview

## Slide 19
lattice heating dynamics
lattice dynamics in graphite

## Slide 20
final lattice temparture from intensity drop: 1227 K
theoretical final temperature (laser fluence 6.7 mJ/cm²): 1135 K
Debye-Waller effect
lattice dynamics in graphite

## Slide 21
ultrafast lattice dynamics
lattice dynamics in graphite

## Slide 22
phonon decay channels
?
lattice dynamics in graphite

## Slide 23
coherenct acoustic phonons
lattice dynamics in graphite

## Slide 24
coherenct acoustic phonons
lattice dynamics in graphite

## Slide 25
coherenct acoustic phonons
lattice dynamics in graphite

## Slide 26
summary
temporal pulse
characterization
lattice dynamics
in graphite
setup and
spatial resolution

## Slide 27
Prof. Dr. Thomas Baumert
Dr. Arne Senftleben
Petra Kasper
Ute Meier-Dietrich
Cristian Sarpe
Silvio Morgenstern
Marlene Adrian
Xaver Holzapfel
Vanessa Sporleder
Hendrike Braun
Nadine Götte
Tillmann Kalas
Jens Köhler
Christian Lux
Jutta Mildner
Stefanie Züllighoven
Dirk Otto
Bastian Zielinski
Dominik Pengel
Thomas Winkler
Philipp Hillmann
Thanks to the group…

## Slide 28
…and thank you very much
for your kind attention !