## Slide 1: Femtosecond low-energy electron diffraction and imaging
A. Paarmann, M. Müller, S. Lüneburg, R. Ernstorfer
Femtosecond Electron Imaging and Spectroscopy
Dec. 11th, 2013

## Slide 2: Acknowledgements
Melanie Müller
Sebastian Lüneburg
Ralph Ernstorfer
FHI Berlin
Max Planck Research Group
“Structural and Electronic Surface Dynamics”
Nanometer Structure Consortium, Lund University
Magnus Borgström
Martin Hjort
Anders Mikkelsen
Lars Samuelson

## Slide 3: Ultrafast Electron Diffraction & Microscopy
Diffraction / Microscopy:
Structural (atomic) resolution
+
time scale: 100 fs
length scale : Å … nm
Pump-probe:
Ultrafast temporal resolution
Transmission
electron diffraction
100 eV
1 keV
100 keV
10 keV
1 MeV
10 MeV
Gas phase
electron diffraction
Relativistic electron diffraction
Reflection high-energy
electron diffraction
Scanning
electron microscopy
Transmission
electron microscopy
Low-energy
electron diffraction /
microscopy
Charge per pulse
Electron energy
+ High surface sensitivity
+/- Very sensitive to electric fields
+ Little sample damage

## Slide 4: Major Challenge at Low Energies: Electron Pulse Duration
Nanotips as electron gun !
Delivering < 100-fs electron pulses at sub-kV energies is a big challenge !
Space charge
Vacuum dispersion
First time-resolved LEED: Karrer, Osterwalder et al., Rev. Sci. Instrum., 72 , 4404 (2001)
4
Time-resolved experiments:
Short propagation time → Compact design
Single / few electron pulses at high rep-rate

## Slide 5: Electron Pulse Duration: Simulations
5
Paarmann et al., J. Appl. Phys. 112, 113109 (2012)
path length difference
dispersion
sample
tip
0.9
0
0
Utip = -200 V
d = 100 mm
E0 = 0.5 eV
Notes: Left Plot:
Sigma = 10°, d=100 um, V=-200 V
Right Plot:
V = -200 V, d = 100 um

## Slide 6: Beam Collimation for Diffraction: ‚Lens Behind the Tip‘
U ≤ -100 V
U > -100 V
Utip = -100 V
Collimation (Focussing) due to plate-capacitor-like field lines
Typically < 5 mm spot size on the sample
suppression of DC field enhancement + current
Disadvantage: dispersive pulse broadening enhanced
Paarmann et al., J. Appl. Phys. 112, 113109 (2012)
Macrolens
Microlens
Lüneburg et al., Appl. Phys.
Lett. 103 , 213506 (2013)

## Slide 7: Experimental Concepts
7
Time-Resolved Low-Energy
Electron Diffraction (trLEED)
Time-Resolved Point Projection Microscopy (trPPM)
Atomic structural dynamics with high surface sensitivity
Ultrafast dynamics in 2D and quasi-2D systems
Ultrafast imaging of nano-scale systems
Spatially resolved probing of
transient electric fields

## Slide 8: Experimental Setup
Ti:Sa oscillator
  80 MHz, 2 nJ, 5 fs
Cavity dumped Ti:Sa
  1 MHz, 30 nJ, 16 fs
Regenerative Ti:Sa amplifier
  200 kHz, few mJ, 50 fs
100 nm
0.18 e-/pulse

## Slide 9: Point Projection Imaging with fs-Electron Pulses
60 nm gold nanowires on quantifoil (2 μm holes)
Laser-triggered emission
DC field emission
Electron energy | 100V
Tip-sample distance | 25 μm
Integration time | 1 s
Laser power | 10 mW
Electron energy | 150 V
Tip-sample distance | 25 μm
Integration time | 0.5 s

## Slide 10: Transmission LEED of single-layer graphene
Unpublished data …

## Slide 11: Space Charge Dynamics
Generate space charge from a metal surface/edge and detect deflection of the probe electron beam
  Pt pinhole
  Cu TEM grid edge
Laser | Coherent RegA | 200 kHz, 50 fs
Pump | Power | 31 mW
 | Fluence | 50 mJ/cm2
Probe | Power | 1.3 mW
Tip-sample distance |  | 300 μm
Electron energy |  | 261 eV
Lens bias |  | -702 V

## Slide 12: Space Charge Dynamics
Unpublished data …

## Slide 13: Space charge dynamics
Unpublished data …

## Slide 14: Transient Electric Fields at Photoexcited Semiconductor Nanowires
time-resolved Point projection microscopy
Semiconducting InP nanowires
  Diameter: 30 nm, length: 1.5 μm
  Placed on quantifoil substrate
Hjort et al., ACS Nano 6, 9679 (2012)
Laser | Cavity dumped | 1 MHz, 16 fs
Pump | Power | 660 μW
 | Fluence | 300 μJ/cm2
Probe | Power | 1.4 mW
Tip-sample distance |  | ~ 20 μm
Electron energy |  | 70 eV
Lens bias |  | -345 V

## Slide 15: Nanowire Local Field Dynamics
Unpublished data …

## Slide 16: Nanowire Local Field Dynamics
Unpublished data …

## Slide 17: Outlook: „Divergent Beam LEED“
Unpublished data …

## Slide 18: Summary
Extremely compact, versatile machine for time-resolved low-energy electron diffraction and microscopy
Large scattering cross section of low energy electrons
  Best suited for low-dimensional systems
  High sensitivity to local electric fields
First observation of real-space local field dynamics at semiconductor nanowires
Resolution in microscopy mode: < 200 fs, ~ 30 nm
Resolution in diffraction mode: < 2 ps, < 0.02 Å-1
Thanks for your attention!